## Slide 1
New Developments and Operating Experiences with High Performance Disc Filters for Tailings Dewatering
www.bokela.com
André Egger
Paste 2016
06/2016

## Slide 2: Economical Dewatering of Tailings with High Performance Disc Filters
Main target of tailings dewatering
recovery of water and make tailings fit for next process step, e.g. mxing with cement for mine backfill
Typical properties of tailings
very fine particles  d50 = 1 micron up to 100 micron
sticky filter cakes  difficult to release from filter fabric
low or high pH value  often corrosive properties
solids content  typically 50 - 70 wt% depending on thickener
clay content  hinders filtration and dewatering
Used dewatering equipment
rotary vacuum disc filters
rotary vacuum belt filters
filter presses
Comparison of
CAPEX and OPEX

## Slide 3: Disc Filter Boozer Installation
the pipes from control head to receivers avoid bends,
tangential receiver inlet minimizes flow restrictions as far as possible
Filter segments
Centre barrel
Control head
Filtrate receiver
Blowback tank
Snap blow valve
Filter trough
Drive unit
2
8
1
6
3
7
5
4

## Slide 4: Focus of Modern Disc Filter Design
Overall pressure loss p(E) – p(A) = min !
A
D
E
C
B
segments
trough
Filtrate pipes
Control head
Piping to receivers
Snap blow valve

## Slide 5: Advantages of BOKELA Disc Filters and Conditions for Use
Modern vacuum disc filters are the perfect choice where following conditions and targets apply
e.g. mine backfill is processed – no pond disposal, dry stacking to be evaluated
the tonnage is > 50 t/h and big filter sizes can be applied
moisture of > 18 wt%
energy efficiency is important
space constraint in the filter building – low footprint required
little operator know how required
highest availability for operation (> 97 %)
water consumption for operation of equipment minimised (average: 1,0 m3/h)

## Slide 6: Dewatering of Gold/Copper Tailings in Bulgaria with Disc Filters after Mine Upgrade
Project Data
Mine backfill project in a gold/copper mine in Europe
Target: reduction of cement added
PSD: d50 = 40 micron
Operational results:
Solids: ms = 110 t/h feed solids = 50 wt-% from thickener underflow
Moisture: mc = 19-22 wt-%

## Slide 7
Moisture Content of Filtered Tailings for Different Copper/Gold Tailings

## Slide 8
Specific Solids Throughput of Different Copper/Gold Tailings versus Filter speed

## Slide 9
Filter 1 and Filter 2
Dewatering of Gold/Copper Tailings in Bulgaria with Disc Filters after Mine Upgrade

## Slide 10: Dewatering of Zinc Tailings with BOKELA Disc Filters
Zinc tailings from a copper and zinc mine in Australia, Qld
Filter: 2 x Boozer ME8 ( 141m² each) replacing 2 disc filters of old design
Target: plant capacity increase from 240 t/h to 350 t/h tailings
PSD: d50 = 50 micron
Solids: ms = 88 t/h
feed solids = 60 - 65 wt-% from thickener underflow
Moisture: mc = 20 – 22 wt-% required

## Slide 11: Dewatering of Zinc Tailings with BOKELA Disc Filters
 |  | Predicted value per filter | Operational value per filter
Solids throughput |  |  | 
normal | [t/h] | 175 | > 175
peek (max.) | [t/h] | 200 | 210
Filter speed for normal operation | [rpm] | 1.5 | < 1
Cake moisture | [wt.-%-%] | 20 - 22 | 17 – 20
Flocculent dosage | [g/t DS] | depending on feed charge | 0 - 50 depending on feed

## Slide 12: Dewatering of Gold/Silver Tailings with BOKELA Disc Filters in 4,800 m Above Sea Level
Mine backfill in a gold/silver mine in Peru
Filter: 2 x Boozer L4 ( 176m² each)
Target: reduction of water content after thickener to allow for mixing with cement
PSD: d50 = 22 - 27 micron
(high clay content)
Solids: ms = 88 t/h
feed solids = 55 wt-% from thickener underflow
Moisture: mc = 23 – 24 wt-% required

## Slide 13
Filter in Operation
Dewatering of Gold/Silver Tailings

## Slide 14
Filter Data |  | BOKELA Boozer Disc Filter | Horizontal Belt Filter | Filter Press
Cake thickness | [mm] | 8 | 10 | 40
Cake formation angle a1 | [°] | 150 | 130 | n.a.
Dewatering angle a2 | [°] | 130 | 150 | n.a.
Filter speed / cycle time | [rpm] / [min] | 0,30 / - | 0.18 / - | - / (25 – 30)
Pressure difference @ vacuum pump | [bar] | 0.45 | 0.45 | 3 feeding / 6 pressing
Comparison of Investment and Operational Cost of Disc Filter, Belt Filter and Filter Press
Solids: ms = 88 t/h, d50 = 25 - 27 micron
Moisture: mc = 20 – 25 wt-% required
Filter adjustment for efficient use of each equipment:

## Slide 15
Filter Data & Operational Results |  | BOKELA Boozer Disc Filter | Horizontal Belt Filter | Filter Press
Filtration area per unit | [m²] | 2 x 176 | 3 x 132 | 4 x 520
Specific solids throughput | [kg/m²h] | >> 250 (up to 330) | 225 | 42
Solids content in feed | [wt-%] | 60 | 60 | 60
flocculents | [g/t] | 30 | 30 | 30
Cake moisture content | [%] | 22 - 23 | 22 - 23 | 19 - 21
Solids throughput per filter | [t/h] | 44 (up to 58) | 30 | 22
Cloth change | [sets/a] | 2 x 12 | 3 x 8 | 4 x 12
Power (filter, hydraulics, compressor, vacuum pump, etc.) | [kwh] | 2 x 110 | 3 x 150 | 4 x 200
Required units for 88 [t/h] | [-] | 2 | 3 | 4
Filter Data & Operational Results

## Slide 16
Operation cost |  | 2 BOKELA Boozer Disc Filter | 3 Horizontal Belt Filters | 4 Filter Presses
Power consumption total | [kW] | 2 x 110 | 3 x 150 | 4 x 200
Specific energy cost | [EUR/kWh] | 0.1 | 0.1 | 0.1
Operation hours | [h/a] | 8000 | 8000 | 8000
Filter cloth exchange | [sets/y] | 2 x 12 | 3 x 8 | 4 x 12
Specific cost for cloth | [EUR/m²] | 30 | 40 | 35
Annual energy cost | [EUR/y] | 176,000 | 360,000 | 640,000
Annual cloth cost | [EUR/y] | 126,700 | 266,100 | 873,600
Flocculent | [EUR/y] | 80,000 | 80,000 | 80,000
Maintenance & spares | [EUR/y] | 36,000 | 45,000 | 160,000
Total operation cost / year | [EUR/y] | 418,700 | 751,100 | 1.753,600
Specific operation cost | [EUR/t] | 0.59 | 1.06 | 2,49
Operation Cost

## Slide 17
Invest cost |  | BOKELA Boozer Disc Filter | Horizontal Belt Filter | Filter Press
Filter cost with receivers and drives | [EUR] | 2 x 750,000 | 3 x 900,000 | 4 x 1,200,000
Auxiliary units with necessary vacuum pumps, compressor, hydraulics etc. | [EUR] | 2 x 200,000 | 3 x 250,000 | 4 x 300,000
Building cost with piping and electrical installation per unit | [EUR] | 2 x 2,375,000 | 3 x 2,875,000 | 4 x 2,500,000
 |  | For all units: |  | 
Total invest cost | [EUR] | 6,650,000 | 12,075,000 | 16,000,000
Invest Cost

## Slide 18: Conclusions
You look for the optimum solution for your tailing treatment
with lowest invest cost?
with lowest operational cost?
Check your conditions!
BOKELA Vacuum Disc filters can be used where following conditions apply
the tonnage is > 50 t/h and big filter sizes can be applied
mine backfill is processed
and/or
moistures of > 18 wt% for the downstream tailing treatment/ storage

## Slide 19
Many thanks for your interest
www.bokela.com